Recovery of Platinum and Palladium in Bi-Component Solutions: Sorption and Desorption

Philippe CHASSARY(1), Thierry VINCENT(1), Lynne MACASKIE(2), Eric GUIBAL(1)

(1)Ecole des Mines d’Alès, Laboratoire Génie de l’Environnement Industriel, 6 avenue de Clavières, F-30319 Alès cedex, France

(2)University of Birmingham, School of Biosciences, Edgbaston, Birmingham, B15 2TT, U.K.

Chitosan has been used as a base material for the preparation of platinum and palladium sorbents. These derivatives were obtained by glutaraldehyde cross-linking (GA), by polyethylenimine grafting (PEI), and by thiourea grafting (TDC). These sorbents have been tested for the recovery of platinum group metals (PGMs) in batch systems and column systems from bi-component solutions at the optimum pH (ca. pH 2). Sorption isotherms have been determined in batch systems considering the impact of the excess of one metal on the sorption of the second metal. The sorbents have a marked preference for palladium over platinum. In most cases, the total sorption capacity (taking into account both Pd and Pt sorption) was comparable to that of metal (indifferently Pd and Pt) in single-component solutions. This indicates that the metals compete for the same sorption sites, regardless of the type of sorbent. In fixed-bed systems, similar trends were observed with typical profiles driven by the displacement of platinum by palladium, because of the greater affinity of sorbents for palladium than for platinum. The sorbents (especially GA and TDC) have a greater selectivity for Pd than for Pt, compared to PEI, which has greater sorption capacities. Desorption was tested using several eluants. None of them allowed the complete removal of the metals from loaded sorbent, nor the selective desorption of one of them. It is difficult to reach a complete separation of the metals.