Poly (acrylamide) grafts on spherical polyvinyl pyridine resin for removal of mercury ions from aqueous solutions

Erdem Yavuz , Bahire Filiz Senkal*, Niyazi Bicak

İstanbul Technical University, Department of Chemistry, 34469, Maslak-İstanbul / TURKEY

E-mail: bsenkal@itu.edu.tr

Poly (acrylamide) was grafted from carboxylic acid groups onto crosslinked quaternized polyvinyl pyridine beads using a redox polymerization methodlogy [1,2].

A beaded polymer with a poly (acrylamide) surface shell was prepared in two steps, starting from poly (vinyl pyridine-divinyl benzene) PVP- DVB (25%) based beads with a particle size of 200- 400 µm; i) quaternization with chloroacetic acid  ii) grafting using a concentrated aqueous acrylamide solution with cerium ammonium nitrate.

The resulting polymeric resin with 116 wt % of grafted poly (acrylamide) has been demonstrated to be an efficient mercury-specific sorbent.

The mercury sorption capacity under non-buffered conditions is around 2.40 mmol .g-1 resin.

[1] H. Bulbul Sonmez, B.F. Senkal, N. Bicak J. Of Polym. Sci., Chemistry ed. 40, (2002)  3068

[2] B. F. Senkal, E. Yavuz, N. Bicak, Macromol. Sym. (2004) (accepted)