EFFECT OF OXIRANE OXYGEN ON THE THERMAL STABILIZATION OF POLYVINYL CHLORIDE

M. T. BENANIBA1 N. BELHANECHE-BENSEMRA2, G. GELBARD3

1 Département de Génie des Procédés, Faculté des Sciences de l’ingénieur, Université de Sétif, 19000 ALGERIE ; e-mail: m_benaniba@yahoo.com

2 Département de Génie de l’Environnement, Ecole Nationale Polytechnique, BP. 182 El- Harrach, Alger, Algeria

3 Institut de recherche sur la catalyse, 6 Avenue Albert Einstein 69626 Villeurbanne cedex, France

Sunflower oil was epoxidized and characterized. Epoxidized sunflower oil (ESO) which was used as an organic thermal co-stabilizer for plasticized polyvinyl chloride (PVC) in the presence of Zn and Ca stearates. The thermo-oxidative degradation of PVC was studied in the presence of this ternary stabilizer system at 170°C. The rates of dehydrochlorination were measured by potentiometric titration and the extents of discoloration were evaluated. The formation of polyene sequences was investigated by UV–visible spectroscopy. The influence of the ratio of Zn and Ca stearates (1/2, 1/1 and 2/1) and of the amount of oxirane oxygen in the ESO were considered. Synergistic effects were found.