Self-Curable Polyester by a Reaction of Glycidol with

Maleic Anhydride

Bunyamin Karagoz, Niyazi Bicak *

Department of Chemistry, Istanbul Technical University, Maslak 34469, Istanbul, Turkey

The controlled reaction of equimolar quantities of maleic anhydride and glycidol in dimethoxyethane gives soluble polyesters with one hydroxyl group in each repeating unit. The reaction proceeds with stepwise ring opening of the components and gives highly viscous clear solutions in relatively short periods. In the first step, monomaleate ester formation takes place around 80 °C.

The ring opening of the oxirane group is the second step, and it occurs at 120 °C. The overall reaction is the formation of soluble polyesters1 with moderate molecular weights (6000-18,000), without the elimination of water. The soluble polyesters can be crosslinked tightly by direct heating at 190 °C without additional vinyl monomer2.

References:

1-)  Hsu, C. P. A.; Lee, L. J. Polymer 1991, 32, 2263.

2-) Grobelny, J. Polymer 1995, 36, 4215.