REMOVAL OF HEAVY METALS BY NOVEL ACRYLIC ION EXCHANGERS

Violeta Neagu, Ion Bunia, Cornelia Luca, Wolfgang H. Holl

The synthesis of some novel chelating acrylic ion exchangers with improved

sorption properties for some heavy metal cations, such as Pb(II), Cd(II), Co(II)

and Zn(II) compared to the commercially available resin, Purolite A-830

were investigated.

Acrylic ion exchangers contain different chelating functional groups as:

acryloamidoethyleneamine, acrylamidotriethylentriamine and hydroxamic acid

+ amidoxime mixture being performed by the aminolysis reaction with

ethylendiamine, triethylentetramine and respective hydroxylamine of

ethylacrylate, acrylonitrile and divinylbenzene copolymer.

The copolymer was performed in the presence of two porogen agents: benzine

and toluene with  view to obtaining two different morphologies of its three

dimensional network.

The ion exchangers synthesised were tested through batch sorption

experiments from metal solutions bearing several heavy metals at initial

concentrations of 0.001 M, 0.005 M and 0.05 M at initial pH value of 5.

The results of the present study demonstrate that the novel

acrylic ion exchangers have favorable properties with respect to the

sorption of heavy metals from waters, which might make them competitive

for commercially available resin.